# CERTIFICATE OF ANALYSIS

## PRODUCT: BOARD DEFENSE

## FORMULA: Na2B8013-4 H2O

Grade: Granular

Lot Number: 2018161

Production Date: 3/14/2018

# Chemical Analysis

### Component		Unit		Specification 		              Result

#### B2O3			%		    67.00		min 		 67.15

#### Elemental Boron 	%		    20.80 	min		 20.85

Na2O			%		    14.00		min		 15.20

Purity 			%		    99.25		min 		 99.47

# Particle Size

Size		US Mesh 	Unit		Specification 		Result

(-) 0.090 mm	 -170		  %		  50.00		min 	 50.20

SHELF LIFE: None. It is a stable chemical and does not undergo any chemical change under the recommended dry and cool storage conditions. However, long exposure to humidity and temperature cycling this product may undergo inter-particle bridging and can form lumps.

50 North 41st Avenue, Phoenix, AZ 85009   Phone: 602-233-0756 Fax: 602-272-4864