### SECTION 1 - CHEMICAL PRODUCT AND COMPANY IDENTIFICATION

| Brand Name | BORON 10® | Manufacturer | InCide Technologies, Inc. |  |  |
| --- | --- | --- | --- | --- | --- |
| Chemical Formula | Na2SO4•H3BO3 |  | 50 N 41st Avenue |  |  |
| Chemical Name/Synonyms | Sodium Polyborate |  | Phoenix, AZ 85009 |  |  |
| Chemical Family | Inorganic Borates | EMERGENCY PHONE NUMBERS |  |  |  |
| CAS/TSCA No. | 183290-63-3 | CHEMTREC |  | 800-424-9300 |  |
|  |  | INCIDE TECHNOLOGIES |  | 602-233-0756 |  |
|  |  | Effective date | August 29, 2022 |  |  |

SECTION 2- TYPICAL PROPERTIES

The following properties are typical of normal production.

CHEMICAL ANALYSIS

|  |  | Typical Range | Standard Specification |  |
| --- | --- | --- | --- | --- |
|  |  |  | Minimum | Maximum |
| Sodium Polyborate | (Na2SO4•H3BO3) | ------ | 99.6% | 100.0% |
| Chloride | (Cl) | 100-600ppm | ------ | 0.04% |

APPEARANCE: 	White powder

ODOR: 		Odorless

PHYSICAL STATE:	Solid

pH AS SUPPLIED: 	7.0 (2.0% solution) @ 25 C

BOILING POINT: 	Not applicable

MELTING POINT: 	171 C

FREEZING POINT: 	Not applicable

VAPOR PRESSURE (mmHg): Negligible@ 20 C SPECIFIC GRAVITY (H2O = 1):  1.4 @ 25 C

SOLUBILITY IN WATER:       Yes (7.46% at 77 F/25 C)

MOLECULAR WEIGHT: 	389.376

ANGLE OF REPOSE: 	horizontal 33 degrees

BULK DENSITY: 		poured (57-65 lb/ft3)

SECTION 3- THEORETICAL PROPERITES

The following properties are textbook theoretical data and are provided for convenience and reference only. These properties are not normally tested for in the commercial product and no representation is made relative to the commercial product.

THEORETICIAL COMPOSITION

| Sodium Polyborate | Na2SO4•H3B3 | 100.00% |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |

pH In Water @ 20oC (68oF)                                                     SOLUBILITY IN OTHER SOLVENTS

| Percent by weight | pH |  |  | oC (oF) | Percent by weight |
| --- | --- | --- | --- | --- | --- |
| 2.0 | 7.00 |  | Glycerol, 99% | 20(68) | 44.8 |

OTHER INFORMATION

Boron #10, also known as sodium polyborate, is a free-flowing, white, crystalline salt.  Boron, the key element in Boron #10, is an essential micronutrient and is present in all foods, particularly fruits, vegetables, grains, and nuts. The average person consumes between one to three milligrams each day as part of a normal healthy diet. Boron occurs naturally in air, water, and soil.

Boron #10 is a neutral inorganic salt often used as an agricultural micronutrient, deodorizer, smolder, and flame retardant.  The LD50 (dose that causes lethality in 50% of laboratory test animals) of Boron #10 is about the same as table salt.  Boron #10 contains no volatile organic components and is used typically as an extender or replacement to boric acid in many applications.

Boron #10 is stable and does not change under normal storage conditions.  Wide fluctuations in temperature and humidity can result in caking.  Care should therefore be taken to avoid such fluctuations during storage of the product.

SECTION 4- PACKAGING AND HANDLING

Granular: 50 lb. (25kg), 100 lb. (50kg) and 2,400 lb. (1,200 kg) multi plastic lined paper bags palletized and stretch wrapped (tote bags for 2,400 lb. lots).  Fifty pound bags per pallet only. It is also available in 2000 lb. semi-bulk bags (1000kg).

Powder: 50 lb. multi wall paper bags.

Information concerning the handling and use of this product is provided in a safety data sheet (SDS).  The SDS must be fully read and understood prior to any exposure, handling, or use of the product.

Information presented herein has been compiled from sources considered dependable and is accurate and reliable to the best of our knowledge and belief, but it is not guaranteed to be so.  Nothing herein is to be construed as recommending any practice or any product in violation of any laws or regulations.  It is the user’s responsibility to determine the suitability of any material for a specific purpose and adopt necessary safety precautions.  We make no warranty as to results to be obtained in using any material and, since conditions or uses are not under our control, we must necessarily disclaim all liability with respect to use of any material supplied by use.

Replaces: January 1, 2020